### Preparing silica bead tubes (Revised 07-12-05)

*It is recommended to wear a mask when weighing Zirconia/silica beads in addition to PPE (safety glasses, lab coat and latex gloves).

- In a weigh boat, measure 15g of 0.5mm Zirconia/silica beads*. Transfer beads into a 50 mL centrifuge tube.

- Using a Kimwipe, delicately wipe sedentary beads from weigh boat into the 50mL tube.

- Weigh 30g of 0.1mm Zirconia/silica beads*. Transfer beads into the same 50mL centrifuge tube. Vortex tube until beads are intermixed.

- Transfer the mixed beads into the designated squeeze bottle, marked “Save for Mixing and Dispensing Beads*.” Swish bottle for further mixing.

- Place a tube rack on the scale and insert a 2mL microcentrifuge tube. Reset the scale by pressing “On/Off” button. Carefully dispense 0.9g of the Zirconia/silica bead mix into the 2mL tube.

- Loosely cap 2mL tube and set aside in silica bead lysis tube rack. Repeat Step 5 until the bead mix is finished. (45g Zirconia/silica beads will fill up ~ 48 tubes)

- Cover top of tube rack with foil and place a strip of autoclave tape. Place the rack on the assigned autoclave cart or give rack to Rick Huang for autoclaving.

- Clean up workstation.

*Bottles with 0.1mm and 0.5mm Zirconia/silica beads and the mixing bottle can be found in the third drawer down, under the sink.